| Content of Data Sheet |  |  |  |  |
| --- | --- | --- | --- | --- |
| Product model | CAB-LC3100A-E-IN / CAB-LC3100B-E-IN |  |  |  |
| Product specification | HSYV-6 4×2×0.52 |  |  |  |
| Test Standard | ISO/IEC11801、TIA-568-C.2 |  |  |  |
| Conductor | Material | OFC(Oxygen free copper) |  |  |
|  | AWG | 24 |  |  |
|  | Nom.O.D.(mm) | 0.52±0.03 mm |  |  |
|  | DC resistance | ≤95 Ω/km |  |  |
| Insulation | Material | HDPE |  |  |
|  | Thickness | 0.2±0.02 mm |  |  |
|  | Diameter | 0.93±0.05 mm |  |  |
|  | Color | Blue/White- Blue | Green/White-Green |  |
|  |  | Orange/White-Orange | Brown/White-Brown |  |
| Pitch | Offset pitch | ≤20 mm |  |  |
|  | Cable pitch | ≤120 mm |  |  |
| Sheath | Material | PVC(complies RoHS/REACH) |  |  |
|  | External O.D. | 5.8±0.3 mm |  |  |
|  | Color | Orange |  |  |
|  | Tensile strength | >13.5 Mpa |  |  |
|  | Thickness | 0.6±0.05 mm |  |  |
| Surface Printing | Letter height | 3.0±0.3 mm |  |  |
|  | Color | Black |  |  |
|  | Print error & Space | 1±0.005 m |  |  |
|  | Case number | Yes |  |  |
| Packing | Packing | Carton |  |  |
|  | Once packing dimension | 420mm*205mm*420mm |  |  |
|  | Twice packing dimension | 450mm*440mm*445mm |  |  |
|  | Twice packing quantity | 2 cases |  |  |
| Packing length | 305±1m |  |  |  |
| Rip-cord | Yes |  | Crossing backbone | Yes |
| Ambient temperature | -20℃～60℃ |  |  |  |